## Slide 1
Physics-based Machining of Aerospace Materials
Dr. Suhas Joshi
Professor, Department of Mechanical Engineering
Indian Institute of Technology Bombay, Mumbai – 400076
Email: ssjoshi@iitb.ac.in

## Slide 2
Introduction
Titanium alloys, their properties and machining difficulties
Theme and Methodology of the work
Chip segment morphology
Mechanics of a chip segment formation
Chip and shear band microstructure
Correlation between machinability and microstructure
Summary and conclusions
Plan of Presentation

## Slide 3
Physics-based Machining
Physics-based Machining refers to understanding -
several microscopic phenomena that occur during machining,
the effect of these phenomena on a chip segment and grain deformation,
the effect on physical and mechanical properties of resulting surfaces,
the consequent machinability or quality of machined surface.

## Slide 4
Physics-based Machining
Chip-tool interface
Intense 2-body / 3-body Friction
Crater wear
Determines position of shear zone
Tool
Work
Shear plane/zone
Largest energy consumer
Strain: 2-8
Temperature: 200 – 1100oC
Strain rate: 103 - 106 s-1
Un-deformed
chip thickness
Chip
Tool – work interface
On Tool
Intense Friction and wear, heat generation
On Work surface
Material separation, severe deformation, machining affected zone.
Machined surface
Flank surface
Face

## Slide 5
High strength-to-weight ratio (Light weight)
Maintains strength at higher temperature of 440 °C
Good corrosion resistance
Compatibility with composites
Inertness to human body
Titanium Alloys Properties

## Slide 6
Alpha | Alpha + Beta | Beta rich alloy
Medium strength Not heat treatable Good creep and corrosion resistance | Medium to high strength Heat treatable and formable | High strength, low ductility Heat and weld treatable Good formability
Alpha alloy
Alpha + Beta alloy
Beta rich (Alpha + Beta alloy)
α+β
Properties of Titanium alloys

## Slide 7
Impeller
Piston
Ultra light weight bolt
Bearing housing
of gas turbine
Fasteners
Airframe structure
Applications of Titanium Alloys

## Slide 8: Properties causing Difficulties in Machining
Low Thermal conductivity
High Reactivity
High strength at high temp.
Segmented chips
Low elastic modulus
High machining temperature
High tool wear
High cutting forces
Chemical wear
Ti alloy 15 W/m °C, Steel 43 W/m °C
Tool melting
Adhesion
Tool breakage
Chatter
Poor surface finish
Ti alloy 110 GPa, Steel 210 GPa
Shear band formation
Cyclic load on the tools

## Slide 9: Theme of Physics-based Machining
Chip segment deformation
Chip segment Morphology
Physics-based Machining
Shear band spacing and thickness
Correlation between microstructural deformation and Machinability
Grain transportation and deformation
Grain deformation in machined surfaces

## Slide 10
Impeller
Piston
Ultra light weight bolt
Bearing housing
of gas turbine
Fasteners
Airframe structure
Applications of Titanium Alloys
www.topcast.it
metallurgyfordummies.com
www.mvagusta.net
www.mvagusta.net
www.mvagusta.net
www.airbus.com

## Slide 11: Orthogonal Machining of Ti64 alloy
Segmented chips
Strain ~ 4 to 6
Strain rates ~ 105/s
Machining Temp
~200 °C to 600 °C 0.5
Shear
bands
Work
piece
Machining
affected
zone
Shear
zone
Tool
Chip
Deformation of grains
Microstructural changes in
  Primary deformation or shear zone
  Machining affected zone
Phase diagram Ti-Al
http://www.calphad.com
Characteristics of machining
Deformation zones in machining

## Slide 12
Distinguishing feature of Ti64 machining
Main characteristic of Ti64 machining are the adiabatic shear bands (ASB)
  Strain ~ 4 to 6
  Strain rates ~ 105/s
  Temp ~200 °C to 600 °C
  Formed in ~ 50
High strain rate ABSs can be also produced by
  1. Orthogonal Machining (OM)
  2. Split-Hopkinson (SH) Experiments on Hat shaped samples
Notes: Possible micro-mechanism:
Shear due to
- dislocation slip
- twinning
- grain boundary sliding
Softening due to:
- high temperature
- strain softening (inverse strain hardening)
- texture evolution
- dynamic recovery
- dynamic recrystallization

## Slide 13
Work
SEM image of chip
Issues in machining titanium alloys (microstructural perspective)
shear
band
a
Optical image of chip
shear
band
Fracture
Shear band
shear
band
Formation of shear band causes
Fluctuation in cutting forces
Non uniform material deformation
Segmented
chip

## Slide 14
Plan of Research
Machining
environment
Processing parameters
Physics of
deformation
in machining
Thermally
enhanced
Room
Temp.
LN2
Speed
Feed
Grain size
Shear band thickness
Spacing between shear band
microstructure machinability
linkage
Segment shape
Segment dimensions
Grain deformation
Input
Output
Compositional
variation
α-alloy
α+β alloy
β-rich alloy
Mist jet

## Slide 15
Epoxy mould
Shear
bands
Work piece
Tool holder
Frozen chip root
Machining affected zone
Quick stop chip freezing device
c. Quick withdrawal
of tool
Mounted sample
Shear
pin
Fulcrum
Quick withdrawal of tool
Insert
Plain strain condition
Four jaw chuck
Thin pipe of large dia.
Cutting edge
larger than pipe
thickness
Tool
Workpiece
93mm
1 mm
Feed
Experimental set up

## Slide 16
Properties of three titanium alloys
α alloy
α+ alloy
 rich alloy
phase
phase
phase
phase
 | Alloy Type |  | 
 | alloy | + alloy | rich () alloy
Properties | Medium strength, Not heat treatable, Good creep and corrosion resistance | Medium to high strength Heat treatable and formable | High strength, low ductility Heat treatable and weldable Good formability, high fatigue strength
Applications | High temperature low strength applications such as gas turbine casing, rings, structural members in hot spots, chemical processing equipment along with cryogenic applications | alloys are used for high strength applications like aircraft gas turbine disks, blades, airframe structural parts, fasteners | High fatigue strength and formability is required such as automobiles, motorcycles, and sports and leisure goods such as golf clubs
 | Alloy Type |  | 
Properties | Medium strength, Not heat treatable, Good creep and corrosion resistance | Medium to high strength Heat treatable and formable | High strength, low ductility Heat treatable and weldable Good formability, high fatigue strength
Applications | High temperature low strength applications such as gas turbine casing, rings, structural members in hot spots, chemical processing equipment along with cryogenic applications |  | High fatigue strength and formability is required such as automobiles, motorcycles, and sports and leisure goods such as golf clubs
Comparative properties and applications of titanium alloys

## Slide 17
SE image of alpha alloy
Grain deformation
before formation
of shear band
Tool
Free chip
surface
Grain
deformation
In between
shear band
Grain
rotation
Shear
direction
Shear band
Highly elongated
grains inside
shear band
Chip
Microstructural evolution in adiabatic shear band
Grains undergo large deformation
Twinning is not observed.
Dislocation slip is dominant deformation mechanism.
Rigid body rotation of grains observed

## Slide 18
IPF
Image quality map
Shear
band
Shear zone
Work piece
Work piece
Tool
Shear direction
Shear
band
Shear zone
Chip
Chip
Microstructural evolution in adiabatic shear band
Region under
consideration

## Slide 19
Grain elongation
and subdivision
EBSD scan
step size 40 nm
Shear band
Shear
band
Shear band
region
Microstructural changes in the shear band
Chip segment
SEM
image
Image
Quality
IPF
Regions surrounding the shear band shows
grains undergo subdivision and deformation
before the formation of shear band.
Magnified image of shear band
Black region showing
deformed grains

## Slide 20
a.
d.
Deformed grains inside the shear band and region of high dislocation density points against dynamic recrystallization
TEM study inside the shear band
Edge of hole made by
twin jet polishing
Shear band
region
Region outside
Shear band
Deformed
grain
Grains with
heavy dislocations
Magnified
image
b.
c.
SAD

## Slide 21
Observation of dislocation density by etch pit method
at shear band region
Polished chip is etched for 10 minute.
A valley formed at the shear band region shows higher material removal from that region.
This indicates shear band region is a strained one with high dislocation density

## Slide 22
 | Experiments in this work | Meyer and Pak (1995,2001,2003) | Perez-prado, Acta mater. Acta mater. 49 (2001) 2905–2917
Observations | No dynamic recrystallized grains are observed in EBSD scan and TEM TEM reveals grains with high dislocation densities in the shear band. Grains surrounding shear band are highly elongated and have shown sub-grain formation | Equi-axed grains with dia. 0.05-0.2 µm. Low dislocation density. Inside shear band, a ring like pattern produced by many crystallographic orientation is apparent. Diahedral angle (~120)at grain boundary triple point indicate that the boundaries have energies consistent with high angles | Cell size 0.2 µm, New dislocation free grains was not observed in TEM, Only dynamic recovery occurred. Appearance of ring like pattern in the center of shear band is not enough evidence for recrystallization. Recrystallization is not observed
Conclusions | No DRX | DRX | No DRX
Comparison of observations with previous TEM studies